Sample Inspection Log (simulated, 1970s, pre-accident)

| Date | Inspection Type | Observation / Notes | Action / Recommendation |
| --- | --- | --- | --- |
| 15 March 1972 | Visual inspection | No visible cracks or surface anomalies | Routine monitoring |
| 20 August 1973 | Ultrasonic testing (UT) | Subsurface anomaly detected (not recognized as critical) | Monitor location; no immediate action |
| 10 May 1974 | Visual inspection | No new surface defects | Routine check |
| 18 November 1975 | Ultrasonic testing (UT) | Small anomaly; micro-cracking possible | Misinterpreted; no immediate corrective action |

Accident Date: 12 Jan 1976 — fractured rail discovered, train halted.

Teaching Notes:

- Inspection failure is realistic: not all anomalies were properly assessed or followed up.

- Allows students to explore interactions between material defects and limitations of inspection regimes.

Material Data (simulated)

Sample ID: Rail-01

Tests / Results / Notes

- Chemical composition: C 0.80%, Mn 0.70%, Si 0.30%, P <0.02%, S <0.02% – within standard rail steel specification

- Hardness: 210 HV – within expected range

- Metallography: Sharp inclusion detected inside the rail cross-section – microscopically irregular iron particle embedded in steel matrix

- Micro-cracking: Tiny cracks initiating around inclusion – localized stress accumulation, no surface corrosion

- Geometry / Dimensional check: Rail profile and dimensions within tolerance – no deviation in shape or alignment

Teaching Notes:

- Students can conclude that the direct cause is not operational misuse, incorrect heat treatment, or geometry, but a material defect (internal inclusion).

- Promotes discussion on manufacturing process, quality control, and monitoring procedures.

- Data can be revealed progressively during the exercise:

  - Start with chemical composition and hardness.

  - Add metallographic observations.

Suggested Use in FTA Exercise

- Initial phase: Students see only partial inspection logs – encourages exploration

- Middle phase: Lab data introduced – guides students toward identifying internal inclusion and production process issues.